Bakelite and Oil

The first consignment of Bakelite sheets was manufactured and QC’d for the Endcap RPCs in week 8 this year 2003. 64 sheets were retained after the QC that involves resistivity and mechanical damage criteria.

This quantity is the minimum necessary to satisfy the requirements of the EDR and beam tests this year. Beam tests are intended to be done by Pakistan, Korea and China.

The cutting was done in week 19 2003

Shipping to CERN and then onto Korea occurred in weeks 20 and 21. The linseed oil also arrived in week 21. The heptane should arrive this week at CERN from Italy and then should leave within 5-10 days to Korea.

Some 10 samples (450mm x 450mm) of this production of Bakelite was expressed to Korea and Pakistan in week 20. These are intended for bonding strength tests with the identical bakelite that will be used to produce the se first pre production gaps.

See our web site under Oil & Bakelite for photos and resistivity results.

More production batches of bakelite will occur in June and July  and then at the end of this year. The contract for the total 1300 sheets is open until April 2004, with reserves on supplementary orders and packing and shipping conditions.

Ian Crotty		4 June 2003