## Slide 1: Malter effect mechanism study in PNPI and MEPhI (Sarov)
G. Gavrilov, M. Buzoveria
28.11.2017

## Slide 2
Study of Malter effect appearance mechanism
e + CF4 → CF3 + F + e; | (1)
e + CF4 → CF3 + F; | (2)
e + CF4 → CF2 + 2F + e; | (3)
e + CО2 → CO + O + e; | (4)
e + CО2 → CO + О; | (5)
e + CО2 → CО + O. | (6)
To remind: CF3, F, O are produced in avalanche at dissociation energy 3  6 eV
O + CF3 → COF2 + F; | (7)
O + CF2 → COF + F; | (8)
e + COF2 → COF + F + e; | (9)
O + COF → CO2 + F . | (10)
Presence of O stimulates additional generation of F which provides etching of Si and other organics
4F + Si → SiF4;
4F + SiO2 → SiF4 + O2;
Si+ CF3 + F + 2O  SiF4 + CO2.
To provide an effective cleaning from silicon and organic deposits a high current about of 20-40 A is needed, that takes
Etching rate can be accelerated with adding O2 in the gas mixture.
This “thin film” or “finger traces” model is well tested at recover of the LHCb muon chambers
Si deposits cleaning by F

## Slide 3
Study of Malter effect appearance mechanism
2 planes, each with 7 controlled anode wires;
50 m gold-coated anode wire;
285 x 340 mm2 sensitive area, 1670 cm3 gas volume;
S = 3 mm ;
L = 4.5 mm ;
Identical geometry and construction materials to CSC ;
Strip resistance control at specially ;
cut strips on the cathode plane ;
Gas flow during aging test was 4 sccm ;
that is  3.5 Volume per day ;
No gas recirculation was applied.
BUT
* Readout from anode wires only ;
* - HV applied to the cathode.
New aging tests are necessary:
due to hard radiation conditions at future HL-LHC
due to first manifestations of Malter effect in CSC
to find eco-friendly solution for CF4 outlet reducing
Small scale CSC prototype module for aging study

## Slide 4: Targeting aging tests in PNPI
First local aging test under 90Sr irradiation was performed with compact CSC prototype module fed by standard CSC gas mixture;
1.36 C/cm accumulated charge is obtained, that is 7× of the expected charge after 3000 fb-1 at HL-LHC. The absence of amplitudes degradation matches with the previous tests in 1999 -2001;
Strip-to-strip resistance dropped during the aging test from 51013  up to 5107 ;
Despite of the strong oxidation and Si coating on cathodes surface, no Malter current manifestation have been found;
Test results can be a benchmark for the future study of the eco-friendly gas mixtures;

## Slide 5
Study of Malter effect appearance mechanism
Irradiation zone on the anode plane 3.7/22.0/2  5.8 cm 2
Along anode wires
Work point set HV=3750 V GG=5104 Ionization current at work point is 17 A per 6 cm2 or
1 A per 1 cm of wire length
1.45106 Hz per 1 cm of wire length
This kind of aging test is actual for longevity evaluation of the CSC modules in extremal conditions and upper estimate of the anode wires aging.
Irradiation zone is a generator of the radicals and ions, which diffuse around in the gas volume of the CSC prototype.
The CSC-CMS comparable damages of the cathode surface in the aged CSC prototype can be found only in the intermediate zone in the not irradiated area.

## Slide 6
SEM image of the copper foil surface of not irradiated FR4
Force microscopy of original FR4
Roughness profile has a depth of 0.4 m

## Slide 7: Study of Malter effect appearance mechanism
Field structure in vicinity of the cathode plane:
…60 m apart from the cathode plane
HV = 3600 kV
HV = 3600 kV
The electric field strength on the CSC cathode planes is ~ 5000 V/cm

## Slide 8
Irradiated zone
Upper cathode plane
Bottom cathode plane
Irradiated spot
Damaged (toughed by oxidation) zone is >>10 times bigger of irradiated spot (~6 cm2)
Main source of cathode aging are the radicals from O2
Q=1.36 C/cm
Q= 0.0 C/cm
Photos of the disassembled detector after accumulation of Q=1.36 C/cm
with 40%Ar+50%CO2+10%CF4
080
103 – 108 m cm
0.01 – 1 m  cm

## Slide 9: Aging results from GIF (1999)
Si
O
Cu
F
D. Acosta et al. NIMA 515 (2003) 226–233
Only left half of the CSC module was irradiated.
Accumulated charge 0.3 C/cm
Oxidation touched both parts of the module

## Slide 10: Targeting aging tests in PNPI
Second aging test under 90Sr irradiation was performed with compact CSC prototype module fed by 36.6%Ar+61.75%CO2+1.65%CF4 gas mixture
0.39 C/cm accumulated charge is obtained
Strip-to-strip resistance dropped during the aging test from 21013  up to 11011 
At accumulated charge ~0.3 C/cm exceeding HL-LHC an appearance of Malter currents was observed
Dedicated studies of the cathode surface are ongoing

## Slide 11
Irradiated zone
Photos of the disassembled detector after accumulation of Q= 0.39 C/cm aged with 36.6%Ar+61.75%CO2+1.65%СF4
Irradiated spot
Q= 0.39 C/cm
Bottom cathode plane
Upper cathode plane
Damaged zone is just
few times bigger
of irradiated spot 8 cm2
Malter current ~100 A was obtained at the end of the tests !

## Slide 12: Study of Malter effect appearance mechanism
Positive ions current and polarised polymers flow is S2/S1 times bigger on the peaks
Due to irradiation, the copper foil on the cathode oxidizes and becomes uneven and rough covering the area bigger of the irradiated zone:
For the test with 10%CF4 (Qtotal  27 C) the damaged (or oxidized) area is 580 cm2 that is ~100 times bigger of the irradiated zone
For the test with 1.6%CF4 (Qtotal  10 C) the damaged (or oxidized) area is 56 cm2 ~ 7 times bigger of the irradiated zone
To extrapolate the cathode foil damage after CSC prototype aging tests on “uniformly” irradiated CSC modules the samples from
not irradiated zone have to be considered
Ions current density through the peak is
j = ji × S/r2 ,
S- peak surface area, r – peak radii, ji - ions flux density.
For cylinder peak j = ji × 2h/r (h – height)
For conical j = ji × ℓ/r (ℓ - length of slope)

## Slide 13
Study of Malter effect appearance mechanism

## Slide 14: CSC CMS prototype longevity test in PNPI
O
EDS mapping and SEM image of sample E small FIB cross section – zoomed 1.
FIB cross section – 5 μm depth milling of sample E
O
EDS – Energy Dispersive X-ray spectroscopy
FIB – Focused Ion Beam

## Slide 15: CSC CMS prototype longevity test in PNPI

## Slide 16
Study of Malter effect appearance mechanism
The physicists from National Research Nuclear University MEPhI ( Sarov) took participation in the study of the samples from the aged CSC Prototype, too …
Cathode FR4 samples from the points E-D, E-D, H, Ef were analysed with
Atomic Force Microscope microscopy with “Solver Next”;
Nuclear scanning microprobe analysis.
«Solver Next»

## Slide 17: Nuclear scanning microprobe setup (EGP-10) - E=14 MeV H+ beam with not less of ±300 µm spot on the target  Scanning rate from point-to-point 200 µs.  Time of positioning less of 40 µs.
1
2
1 – Ions optical focusing system; 2 – beam-sample interaction chamber

## Slide 18: Reference point C
Force microscopy analysis of the surface structure
Evaluation of surface roughness
Detection of micro damages on the surface - blisters

## Slide 19
Sample E-D from intermediate zone
90 ×90 m
3 × 3 m
The blisters are often formed on the traces of machining, along the boundaries of structural formations. This photo is typical for the described case. Vesicles (blisters) are formed along the fibres
E-D

## Slide 20
Surface profile along ~120 m line
Roughness
90 × 90 m areas
1.0 m
0.12 m
Sample E-D
Roughness varies greatly even within the same sample and increase toward the irradiation zone

## Slide 21: Sample E-H
A crater after blister explosion
3 × 3 m
E-H

## Slide 22: Sample Ef
Sample H
Ef
H

## Slide 23
а
б
с
Sample C - porosity evaluation procedure
a
b
c
d
image preparation for processing;
pore release;
result;
resulting histogram.
«Grain analysis» program

## Slide 24
Porosity distribution in the samples
Sample
Histogram
Histogram
Sample
Area of porous space, %
Area of porous space, %
140
120
18
100
200
Most of porous has diameter 1.0-1.5 m
In the “reference” point C the porous size is smaller then in the rest samples - 0.7 m
500

## Slide 25
Chart: Depth in the cooper foil, m
| 4 | 4.7 | 5 | 6.1 | 6.4 | 6.8 | 6.9 | 7
E-D__Cu | 10 | 20 | 40 | 50 | 60 | 80 | 90 | 100
E-D__Oxygen | 90 | 80 | 60 | 50 | 40 | 20 | 10 | 0
Chart: Depth in the cooper foil, m
| 3.8 | 4.5 | 4.8 | 5.2 | 6
Ef__Cu | 10 | 33.3 | 50 | 66 | 100
Ef_O | 90 | 66.6 | 50 | 33.3 | 0
Ef
H
Chart: Depth in the cooper foil, m
| 4.34 | 5.44 | 6.08 | 6.9300000000000024 | 8.5
E-H__Cu | 10 | 30 | 40 | 50 | 100
E-H_Oxygen | 90 | 70 | 60 | 50 | 0
E-H
E-D
Nuclear scanning microprobe analysis of the samples
Chart: Depth in the cooper foil, m
| 5.5 | 7 | 7.7 | 8.5 | 9.1 | 10
H___Cu | 10 | 20 | 50 | 70 | 80 | 100
H___Oxygen | 90 | 80 | 50 | 30 | 20 | 0
Vary of concentration of the Oxygen in the Cooper foil with a depth of the analysed layer
for different samples
Oxygen concentration changes from 90% at the 3 m surface layer up to 0% on the 6-10 m depth in the cooper foil

## Slide 26: Summary & Outlook
Oxygen radicals and molecules play a key role in the damage of the cathode copper causing the blisters grow and roughness increase
At early stage of Сu oxidation (Cu2O - cuprous oxide ) when surface resistance is high an appearance of Malter current is very probable
While the cooper oxidation continues up to the conductive CuO - cupric oxide - the probability of Malter effect decreases
An accurate surface resistance measurement is needed for the samples of aged CSC prototypes
More systematic study of the damaged cooper foil with an atomic force microscopy and microzond is planned

## Slide 27: Backups

## Slide 28
Sample E-H
Optical microscope image
SEM image
Optical microscope image
SEM image
Backups

## Slide 29: Nuclear scanning microprobe analysis with EGP-10
θ = 180 - θ2 ;
Considering the kinematics of the collision (that is, the conservation of momentum and kinetic energy), the energy E1 of the scattered projectile is reduced from the initial energy E0: E1 = K() × E0 , where K() is known as the kinematical factor,
To measure backscattered energy the Si surface barrier detector is used.
Ions which reach the detector lose some of their energy to inelastic scattering from the electrons. Number of electron-hole pairs produced in the detector is dependent on the energy of the ion.

## Slide 30
L. De Los Santos Valladares et al., Crystallization and electrical resistivity of Cu2O and CuO obtained by thermal
oxidation of Cu thin ﬁlms on SiO2/Si substrates, Thin Solid Films 520 (2012) 6368–6374

## Slide 31
Flora M. Li et al., Low temperature (<100 °C) deposited P-type cuprous oxide thin ﬁlms: Importance of controlled oxygen and deposition energy, Thin Solid Films 520 (2011) 1278–1284
Copper forms two types of oxides: cuprous oxide (Cu2O) and cupric oxide (CuO), each with unique material properties as highlighted in Table 1. Cu2O is a highly transparent, yellow, p-type semiconductor, while CuO is typically an opaque, more conductive material. Although Cu2O is the native oxide of copper, it is often difﬁcult to form pure Cu2O ﬁlms and requires precise control of the stoichiometry. Even moderate excess of oxygen and/or reaction energy tends to favour the formation of CuO instead of Cu2O. Fig. 1 provides a simpliﬁed illustration of the oxidation pathway to form Cu2O and CuO from copper.