## Slide 1: 2nd step to study qualitativily the optical transmission of HPL
Ian
20 Jan 2020
Input from P. Vitulo

## Slide 2
Different light source and lighting conditions
Neon Florescent Tube
Sun with reduced reflection from operator side

## Slide 4
RE1/1 Bot Gap
RE1/1 Top Wide Gap
RE Cut Top Wide Gap No ID
Three samples that are from the RE1, 2 and 3 stations production.
Very close in the production run

## Slide 5
RE4/2 ? Top Wide Gap

## Slide 6
RE4/2 Bot Gap
No ID

## Slide 7
Neon Florescent light tube
4000k
XXXWatts

## Slide 8
Tube source under the HPL in day light and at night
The blinding neon tube and the red transmission through the HPL

## Slide 10
2 dark bands are visible. There is an indication of higher transmission at the high “R” end (The yellow tape)
More light is transmitted in the centre of the panel rather than the top and bottom edges due to the greater thickness through which the light must travel to the camera ??

## Slide 11
The piece of yellow tape.
Bottom RH corner.

## Slide 12
RE4/2 ? Top Wide Gap

## Slide 13
RE4/2 ? Top Wide Gap

## Slide 14
The earlier HPL is less transparent .
RE1/1 bottom panel
In day light on the left And in the dark with the light on in the dark on the right

## Slide 15
Cheap Nikon camera, very slight transmission
Smart phone taking a picture of the Nikon before the exposure is taken and the HPL is more luminous. The cameras have firmware that adjusts the photograph to make “the best shot” which is not necessarily what we want here.
RE type2 Cut Top Wide Gap No ID

## Slide 16
Revert to the sun as a broad band intense and uniform light source but with reduction of the back reflection from “behind” the HPL

## Slide 17
Looking through the small aperture at the HPL on the other side of the box that is facing the sun. The box is not light tight !
The uniformity is far better than what has been observed so far, the piece is however small.
RE1/1 bot gap mounted on a nominally light proof box
Aperture on the opposite face of the box for the camera.
Nikon Camera
Samsung A50

## Slide 18
RE Cut Top Wide Gap No ID
Slight cloud but little attenuation , especially in the red ?
The bright spot above, in the middle is the slit above the camera allowing light to enter and be reflected off the panel.
Samsung A50
Nikon Camera

## Slide 19
RE4/2 ? Top Wide Gap
Here the intensity is greater than the older samples. Perhaps a greater degree of dispersion is evident. The light streak on theLHS and the dark edges on the RHS and top.
The intense source
Samsung A50
Nikon Camera

## Slide 20
Unfortunately the largest panel was not put into a similar arrangement as a bigger box would be required. 2m x 1m x 1m

## Slide 21
The specification of the light proof box.
The aperture angle necessary to cover the entire HPL sheet was achieved with a distance between the sheet and the camera, measured for both cameras and established at > 1420mm.
The dimensions of the HPL sheet are shown, with the aperture for the camera in the rear face.
Fortunately a suitable box was found with our CSC colleagues and kindly leant for this trial.
Dimensions; 2600 x 1370 x 1100mm. A little small on the width.

## Slide 22
The box modification.
Open up the necessary apertures, HPL and camera.
Counter weight to allow the ready movement of the large box.
HPL opening
Camera access on the opposite face
Counter weight ~ 180kg
Distance from HPL to Camera is just sufficient to cover the full length of the RE type 2 bottom HPL panel

## Slide 24
Results, qualitative so far

## Slide 26
Conclusion
The neon light gives a good idea of the transmittance over a long narrow section of the panel. It’s intensity is insufficient with the Nikon camera available.
There are different sensitivities of cameras and phone based cameras. A good knowledge of their operation is necessary. Choose a good smart phone !
The sun is very good when it is visible and there is no cloud movement.
Alternative light sources (Neons, LEDs etc) that are more readily available at least in this part of Europe during winter could be chosen.
The HPL panel is not homogeneous in light transmission. Assuming a correlation between the transmission and the panel composition it is clear that there are “streaks“ of non uniformity along the length of the HPL panel. As they are along the length , panel length ~ 1.7m which forces the length of the RE2 Bot panel to be orientated along the length of the HPL that is 3.2 x 1.6m approx, then they could be produced by the production of the kraft paper sheets. This then implies that the rollers of the machine running the paper through the phenolic resin are not producing a homogeneous pressure across the paper. Possibly there could be a non homogeneous mixture of resin in the bath the paper goes through but given the speed of this process I would assume that there is mixing action given by the movement of the paper alone.
Can this principle be used as a Quality assurance instrument ? It would require some form of digitising to allow analysis.
There is still no correlation between the conductivity and transparence.
And in addition no correlation between variation of transmission or conductivity and density
We are waiting for Pakistan to return the resistivity tool. An alternative could be built.

## Slide 27
Appendix
Camera types
Light sources

## Slide 28
This document can be found here;
http://project-cms-rpc-endcap.web.cern.ch/project-cms-rpc-endcap/rpc/Production/Oil%20&%20Bakelite/Quality/Transparency/2ndStepQualitativeHPLOpticalTransmission.pptx
The previous document is here;
http://project-cms-rpc-endcap.web.cern.ch/project-cms-rpc-endcap/rpc/Production/Oil%20&%20Bakelite/Quality/Transparency/TranparencyHPL6Jan2020V2.pptx
Paolo’s comment
Sources Light;
http://project-cms-rpc-endcap.web.cern.ch/project-cms-rpc-endcap/rpc/Production/Oil%20&%20Bakelite/Quality/Transparency/TransmissionWaveLengthSources.pptx
All photos;
http://project-cms-rpc-endcap.web.cern.ch/project-cms-rpc-endcap/rpc/Production/Oil%20&%20Bakelite/Quality/Transparency/Photos/