# Bakelite and Packing paper Density

## Bakelite

A production piece cut from an edge of a sheet 3.2m by 1.6m

Dimensions 		460 x 221 x 2mm = 203320mm3

= 203cm3

Weight measured 	=	290g

Density		=	290/203

= 	1.4285 g/cm3

Specific Density		0.2857g/cm2

= 	2.857kg/m2

Sheet Weight 		1.6m x 3.2m

=	14.63kg

Kraft Paper

Kraft Paper Density		16g/ 460 x 230 x 0.22mm

=	0.687 g/cm3

Specific Paper density		=  151.2g/m2

I. Crotty 5 Nov. 2003