CONSTRUCTION DETAILS

2x0,22 15 KV DC

Conductor     	: 	nomin. sect.   0.22 mm2 tinned copper 7X0,20 mm

cond. diam. 0.60

Conductor shield	: 		conductive compound PE base

nominal diameter 1.00 mm

Insulation    	: 	Low density polyethylene, colours 1 natural, 1 natural with

white trace

nominal diameter 2.70 mm

2x0,22 signal return

Conductor     	: 	nomin. sect.   0.22 mm2 tinned copper 7X0,20 mm

cond. diam. 0.60

Insulation    	: 	Low density polyethylene colour black

nominal diameter   1.80 mm

Assembly      	: 	conductors twisted in star quad

diameter over assembly 5.4 mm

Wrapping      	: 	Al/polyester tape as flame barrier

Overall Shield 	: 	tinned copper braid

wire diameter 0.10 mm. cover. dens. nom. 85%

Outer sheath   	: 	Thermoplastic LS0H flame retardant compound                   		colour RED RAL 3000

nominal diameter   7.35 mm, 7.50 mm Max.

Marking       	: 	“1x(2x0,22+2x0,22)H2M1 15 KV CC IEC 60332-1 NOVACAVI MILANO

year”

------------------------------------------------------------

ELECTRICAL AND PHYSICAL CHARACTERISTICS

Electrical resistance sect.: 0.22 < 90.900 ohm/km at 20°C

Insulation resistance   >    1000 Mohm x km at 20° C

Test voltage (0,22 15 KV DC)      12  kV ac x 1 min

Test voltage (0,22 signal return) 1,5 kV ac x 1 min

OTHER CHARACTERISTICS

Weight :   76 kg/km

Bending radius static           :   50 mm

Working temperature range       : from   -30 to +80   °C

REFERENCE STANDARDS

IEC 60332-1, CERN IS 23 exluding radiation resistance for sheath