## Slide 2
CHARM facility Layout
For more details, the CHARM web site: http://charm.web.cern.ch
HV connector placed in Pole 1 of the Charm facility during one week
24-31 /10/2018

## Slide 3
Dose (Gy) | HEH Fluence (cm-2) | 1MeV n eq. (cm-2) | Total POT*
103 | 2.83·1011 | 2.71·1012 | 1.4·1016
Here are the dose reached during the irradiation of the HV connector :
The reference document related to the irradiation test: https://edms.cern.ch/document/2048697/1
Max dose in R3,4/1 : 45 Gy for 3000 fb-1
Thanks to Salvatore Danzeca and Chiara Cangialosi of the Charm facility Group who took care of the irradiation test

## Slide 4
Preliminary measurement done by Atlas colleagues.
They think it is sufficient to assess the insulator did not suffered from the irradiation.
They are completing the measurement in more details.
Naked : connector left open in the air
Covered : connector close by insulator